## Slide 1: Resonant Inelastic X-ray Scattering Study of Electron-Exciton Coupling in high-Tc cuprates
F. Barantani,1,2 M. K. Tran,1 I. Madan,2 I. Kapon,1 N. Bachar,1 T. C. Asmara,3 E. Paris,3 Y. Tseng,3 W. Zhang,3 Y. Hu,4,5 E. Giannini,1 G. Gu,6 T. P. Devereaux,5,7,8 C. Berthod,1 F. Carbone,2 T. Schmitt,3 and D. van der Marel1
1Department of Quantum Matter Physics, University of Geneva, 1211 Geneva, Switzerland
2Institute of Physics, École Polytechnique Fédérale de Lausanne, Lausanne, 1015, Switzerland
3Photon Science Division, Paul Scherrer Institut, 5232 Villigen PSI, Switzerland
4Department of Applied Physics, Stanford University, CA 94305, USA
5Stanford Institute for Materials and Energy Sciences, SLAC,CA 94025, USA
6Brookhaven National Laboratory, Upton, NY 11973 5000, USA
7Department of Materials Science and Engineering, Stanford University, Stanford, CA 94305, USA
8Geballe Laboratory for Advanced Materials, Stanford University, CA 94305, USA
Geneva, September 16th 2022

## Slide 2: High temperature superconductors: quick overview (from last 40 years)
Changing the carrier concentration:
many different ground states
(AFM, SC, pseudogap, strange metal, Fermi liquid,...)
Interplay between competing interactions
(t)
(U)
Itinerant
electrons
Localized
electrons
Spin interaction
(for large U)

## Slide 3
Although this may seem a paradox, all exact science is dominated by the idea of approximation.
(Bertrand Russel)
Symmetry is what we see at a glance. (B. Pascal)
Low energy
High energy
Common threads in physics
Renormalized low energy physics
Is it legit?
antiferromagnetism
symmetry breaking in superconductivity

## Slide 4: Technicalities (I)
ADRESS @ SLS (PSI, Switzerland)
square lattice with one electron per Cu atom in
Bi
Ca
Sr
O
Cu
Approximation!
This is the hole doping
real crystal: Bi2Sr2CaCu2O8-x
Cu-O planes

## Slide 5: Technicalities (II)
ADRESS @ SLS (PSI, Switzerland)
Cu
photon in
photon out
Crystal field levels
dd excitons
Resonant inelastic x-ray scattering (RIXS)
RIXS spectrum
crystal
We measure the
energy loss
[photon energy ∼1keV]

## Slide 6: Signature at the superconducting temperature
Energy center of mass
OD
OP
UD

## Slide 7
“normal” (T>Tc) state: AFM local order
Temperature
Tc
superconducting state (T<Tc): spin singlet pairing
underdoped
overdoped
normal (T>Tc) state: more Fermi-liquid like (no spin fluctuations)
‘ordered’ phase
‘disordered’ phase
Cooper’s pairs
Doping
‘less-ordered’ phase

## Slide 8
Phase diagram with exciton energy
UD
OD
OP
Exp SC-induced effect

## Slide 9
P. W. Anderson, Science 316, 1705 (2007)
F. Barantani et al.,
Phys. Rev. X 12, 021068 (2022)
Coupling of high energy excitations (≈ 2 eV) to low energy physics (SC ≈ 20 meV )
Cooper’s pairs and dd excitons and involve the same electrons
The “order” of the spin system changes in opposite directions for UD and OD when crossing the superconducting transition
Conclusions
Maybe we have to question our approximations…

## Slide 10
Thank you for your attention!

## Slide 11
Resonant Inelastic X-ray Scattering
Parameters:
X-ray energy (resonant at Cu-L3 edge)
Polarization (𝜎)
Momentum transfer ()
BZ direction (nodal and antinodal)
Temperature
L. J. P. Ament et al., Rev. Mod. Phys. 83, 705 (2011).
photon in – photon out technique
probe collective modes at finite momentum q
elemental specific (Cu in our case)
2p
2p
E
E

## Slide 12
“normal” (T>Tc) state: AFM local order
T
Tc
SC (T<Tc) state: spin singlet pairing
underdoped
overdoped
SC (T<Tc) state: spin singlet pairing
normal (T>Tc) state: more Fermi-liquid like
(no spin fluctuations)
=
N
SC
=
N
SC

## Slide 13
dd excitons
Localized orbital excitations on the Cu site (dipole forbidden)
No change in site occupancy: no energy cost of order U, so the energy corresponds to splitting due to the crystal field [23, 24]
Robust against doping: excitons in the AF insulator region.
Moretti Sala et al. (2011) New Journ. Phys., 13(4), 043026
eg
t2g