## Slide 1: Ionic gating with Li-ion conductive glass ceramics
Margherita Melegari
16th September
Young Research Day 2022

## Slide 2
Temperature [K]
Magnetic Field [T]
Carrier Density [cm-2]
Field Effect Transistor
First FET was made in 1959 with a solid-state dielectric (SiO2)
Through the application of an electric field, it can tune charge density inside a material
Unable to reach high carrier densities (only up to 1013 cm-2 ), due to the breakdown
voltage limitation of silicon oxide dielectric
The role of FETs in fundamental studies
Carrier density influences the conductivity and the electronic phase of a material, giving us the possibility to play with
it in order to go far beyond the borders of classical physics
G
D
S
SiO2

## Slide 3
Ionic Gating
Liquid Electrolyte
Able to reach carrier densities up to 1014 cm-2 thanks to the formation
of an electric double (EDL) at the surface with the gated material
What is this EDL?
Under the action of an electric field, mobile ions present in the electrolyte accumulate close to the gated material creating a nanocapacitor of 1nm thickness
This allow us to easily tune the charge density, thanks to the capacitance values in the order of mF, a magnitude larger with respect to normal solid-state dielectrics
The technique is cumbersome, due to the liquid phase of the electrolyte
The IL covers completely the device surface, hindering the possibility to use further techniques
What about a solid Electrolyte?

## Slide 4
Lithium-Ion Glass Ceramics
Solid oxide framework with mobile alkali ions (Li+) with high ionic conductivity (10-3/10-4Scm-2)
Manly used as a component in batteries
Stable in ambient condition
Mean roughness around 1nm
Formation of an EDL at the surface with the gated material
VG>0 Li + move to the gated material, VG<0 ion movement to the gate electrode (depletion region at the surface)
Silicon oxide underneath the metal contacts in order to protect them from faradaic reaction with Li ions

## Slide 5
Ionic Gate Spectroscopy
Band gap
Ref-NL
Ref-L
Monolayer WSe2
Large geometrical capacitance together with the implementation of a local reference electrode allow us to measure the bandgap of a semiconductor directly from the transfer curve
Holes
Electrons

## Slide 6
Gate induced Superconductivity
LICGC allows to accumulate a density of charge in excess of n1014 at which MoS2 becomes superconductive
3L MoS2
Tc
Ic
T>Tc
Also, the Temperature T[K] and the Magnetic Field [B] play a role in the suppression of the superconductivity phase
How to transform an insulator in a perfect conductor?

## Slide 7
Summary
We implemented a new Ionic Gating technique based on Solid Electrolyte (LICGC) in order to study new physical phenomena tuning easily charge density
Thanks to new technical improvement, we can reach large EDL capacitance which allows us to perform spectroscopy experiments on 2D semiconductors
Furthermore, also a high carrier density up to 1014 cm-2 can be reached, which can transform a simple semiconductor in a superconductor

## Slide 8
Acknowledgment
Alberto Morpurgo
Chuan Wu
Cao
Ignacìo
Gutiérrez-Lezama
Daniil Domaretskiy
Marc Philippi